•	specifications
	◦	content: 100% Polyurethane
	◦	backing: 43% Recycled Leather; 40% Polyester;
	◦	  17% Cotton
	◦	weight: 24.96 oz / lin. yd. (773g/M)
	◦	width: 54”
	•	environmental friendly benefits
	◦	✓ PVC free
	•	Hide Full Specifications 
	•	performance
	◦	abrasion:
	◦	Heavy Duty – Exceeds 100,000 Cycles
	◦	(Wyzenbeek – Cotton duck Abradant) (ASTM D4157)
	◦	 
	◦	light fastness:
	◦	Class 4/100 hrs. min. (AATCC16A)
	◦	 
	◦	color fastness:
	◦	Class 4 (ASTM D3597, AATCC 8) Wet
	◦	Class 4 (ASTM D3597, AATCC 8) Dry
	◦	 
	◦	physical properties:
	◦	Class 4 (ASTM D3511) Brush Pill
	◦	94 warp, 79 lbs. weft (ASTM D4034) Breaking Strength
	◦	18 warp, 16 lbs weft (ASTM D2262) Tear Strength
	◦	37 warp, 44 lbs. weft (ASTM D4034) Seam Slippage
	•	flammability
	◦	passes:
	◦	California Tech. Bulletin #117 Section E (CS-191-53)
	◦	UFAC Class 1
	◦	NFPA 260 Class 1
	◦	MVSS 302
	•	care
	◦	cleanability:
	◦	W – Water based cleaners may be used
	•	
Pattern images shown up the roll.

Due to pattern scale and color variations in computer monitors and printers, we strongly suggest you view actual samples before making a selection.